Quality Engineering Management Table

| Lost Wax Casting Process (investment casting) | Doc. No. | 4-02-001 | Date: | 2002.11.30 |  |  | Version: 1 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Works | Management items | Management method | Ref. documents |
| No. | Station |  | Item | Quality request | Method/equipment | Timing | Duty | Inspection record | Check basis |
| 1 | Incoming material Inspection | As per “Incoming material inspection control standard” | 3-10-001 |
| 2 | Material in stock | As per “Moving, saving and packing management” | 2-15-001 |
| 3 | Dissolve and add wax |  | Wax quality | Clean | Visual | Once/ 2 weeks | Worker leader | Yes | 4-09-003 |
| 4 | Wax injection bar |  | Surface of wax bar | Smooth | Visual | Full | Worker | No | 3-08-003 |
| 5 | Wax injection |  | 1、Letters | Clear, Correct | Visual | Full | Worker | No | Process control chart |
|  |  |  | 2、Appearance | No bubble, Smooth | Visual | Full | Worker | No |  |
|  |  |  | 3、Internal holes | No deformation | Visual | Full | Worker | No |  |
|  |  |  | 4、Q’ty | Process control chart | Calculation | Per lot | Worker | Process control chart | Process control chart |
|  |  |  | 5、Pressure | Process control chart | Wax injection pressure chart | Per lot | Worker | Process control chart | Process control chart |
|  |  |  | 6、Temperature | Process control chart | Wax injection temperature chart | Per lot | worker | Process control chart | Process control chart |
|  |  |  | 7、Time of wax injection | Process control chart | Time table of wax injection | Per lot | Worker | Process control chart | Process control chart |
| 6 | Wax repair |  | Burrs | De-burrs | Visual | Full | Worker | No |  |
| 7 | Pattern assembly |  | 1、Correct way for wax bar and pattern assembly | Wax pcs assemble smoothly to wax bar joint | Visual | Full | Worker | No | Process control chart 3-08-003 |
|  |  |  | 2、Material mark | Correct | Visual | Full | Worker | No | Process control chart 3-08-004 |
|  |  |  | 3、Q’ty calculation | Correct | Visual | Full | Worker | No | Process control chart |
| 8 | Hanging and clean wax pcs |  | 1、Hanging | Iron slice stay close to wax bar | Visual | Full | Worker | No |  |
|  |  |  | 2、Clean wax pcs | Clean fully | Visual | Full | Worker | No |  |
| 9 | Dipping |  | 1、Concentration | 28-30secs | Stop watch and No.5 glass | Once/day | Worker leader | Shell temperature, humidity and thick liquid concentration check list | 3-08-005 |
|  |  |  | 2、Concentration | 30-32secs | Stop watch and No.5 glass | Once/day | Worker leader | Shell temperature, humidity and thick liquid concentration check list | 3-08-005 |
|  |  |  | 3、Concentration | 10-12secs | Stop watch and No.5 glass | Once/day | Worker leader | Shell temperature, humidity and thick liquid concentration check list | 3-08-005 |
| 10 | Wax removal |  |  |  |  |  |  |  |  |
| 11 | Open furnace and material analysis |  | 1、Shell Physics test | No | No | Process control chart | Worker leader | No | 2-08-002 |
|  |  |  | 2、Temperature of pouring | Process control chart | Temperature tester | Per furnace | Worker | Process control chart | Process control chart |
|  |  |  | 3、Material analysis | As per specification | Spectrometer | Per furnace | QC | Spectrometer list | 3-08-006 |
| 12 | Casting shake out Marking & tracking |  | Heat No. | Clear, Correct | Visual | Per furnace | Worker | 4-10-004 | 3-07-001 |
| 13 | Sand blasting |  | Surface roughness | Smooth | Visual | Full | Worker | No |  |
| 14 | Gate cut off、Heat treatment、Physics property test |  | 1、Heat treatment | As per specification | Microscope | As per customer’s request | QC | Heat treatment report | 3-08-008 |
|  |  |  | 2、Physics property | As per specification | Tensile and Impact tester | As per customer’s request | QC | Tensile and impact report | 3-08-006 |
| 15 | Grinding |  | In gate grinding | Moderate height | Visual | Full | Worker | No |  |
| 16 | Acid wash |  | Change acid liquid | Shine | Visual | Daily | Worker |  | 4-08-006 |
| 17 | Final Inspection |  | 1、Appearance of casting | Clean, complete | Visual | Full | QC | Final inspection daily report |  |
|  |  |  | 2、Internal of casting | No shrinkage and defect | Visual | Full | QC | Final inspection daily report |  |
|  |  |  | 3、Letters of heat no. | Correct and Complete | Visual | Full | QC | Final inspection daily report | Process control chart |
|  |  |  | 4、Dimensions check | As per customer’s drawing | Caliper and Height gage | As per customer’s request or new molding | QC | 4-10-002 | Customer’s drawing and Incoming material inspection control standard |
|  |  |  | 5、P.T. | DIN 1690-2 | P.T. reagent | As per customer’s request | QC | 4-10-005 | DIN 1690-2 |
|  |  |  | 6、X-ray | DIN 1690-2 | X-ray tester | As per customer’s request | QC | 4-10-006 | DIN 1690-2 |
| 18 | Repair |  |  |  |  |  |  |  |  |
| 19 | Packing and Delivery |  |  |  |  |  |  |  |  |