Quality Engineering Management Table

| Lost Wax Casting Process (investment casting) |  |  | Doc. No. |  | 4-02-001 |  | Date: | 2002.11.30 |  |  |  |  |  | Version: 1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Works |  |  |  | Management items |  |  | Management method |  |  |  |  |  |  | Ref. documents |
| No. | Station |  |  | Item |  | Quality request | Method/equipment |  | Timing | Duty |  | Inspection record |  | Check basis |
| 1 | Incoming material Inspection | As per “Incoming material inspection control standard” |  |  |  |  |  |  |  |  |  |  |  | 3-10-001 |
| 2 | Material in stock | As per “Moving, saving and packing management” |  |  |  |  |  |  |  |  |  |  |  | 2-15-001 |
| 3 | Dissolve and add wax |  |  | Wax quality |  | Clean | Visual |  | Once/ 2 weeks | Worker leader |  | Yes |  | 4-09-003 |
| 4 | Wax injection bar |  |  | Surface of wax bar |  | Smooth | Visual |  | Full | Worker |  | No |  | 3-08-003 |
| 5 | Wax injection |  |  | 1、Letters |  | Clear, Correct | Visual |  | Full | Worker |  | No |  | Process control chart |
|  |  |  |  | 2、Appearance |  | No bubble, Smooth | Visual |  | Full | Worker |  | No |  |  |
|  |  |  |  | 3、Internal holes |  | No deformation | Visual |  | Full | Worker |  | No |  |  |
|  |  |  |  | 4、Q’ty |  | Process control chart | Calculation |  | Per lot | Worker |  | Process control chart |  | Process control chart |
|  |  |  |  | 5、Pressure |  | Process control chart | Wax injection pressure chart |  | Per lot | Worker |  | Process control chart |  | Process control chart |
|  |  |  |  | 6、Temperature |  | Process control chart | Wax injection temperature chart |  | Per lot | worker |  | Process control chart |  | Process control chart |
|  |  |  |  | 7、Time of wax injection |  | Process control chart | Time table of wax injection |  | Per lot | Worker |  | Process control chart |  | Process control chart |
| 6 | Wax repair |  |  | Burrs |  | De-burrs | Visual |  | Full | Worker |  | No |  |  |
| 7 | Pattern assembly |  |  | 1、Correct way for wax bar and pattern assembly |  | Wax pcs assemble smoothly to wax bar joint | Visual |  | Full | Worker |  | No |  | Process control chart 3-08-003 |
|  |  |  |  | 2、Material mark |  | Correct | Visual |  | Full | Worker |  | No |  | Process control chart 3-08-004 |
|  |  |  |  | 3、Q’ty calculation |  | Correct | Visual |  | Full | Worker |  | No |  | Process control chart |
| 8 | Hanging and clean wax pcs |  |  | 1、Hanging |  | Iron slice stay close to wax bar | Visual |  | Full | Worker |  | No |  |  |
|  |  |  |  | 2、Clean wax pcs |  | Clean fully | Visual |  | Full | Worker |  | No |  |  |
| 9 | Dipping |  |  | 1、Concentration |  | 28-30secs | Stop watch and No.5 glass |  | Once/day | Worker leader |  | Shell temperature, humidity and thick liquid concentration check list |  | 3-08-005 |
|  |  |  |  | 2、Concentration |  | 30-32secs | Stop watch and No.5 glass |  | Once/day | Worker leader |  | Shell temperature, humidity and thick liquid concentration check list |  | 3-08-005 |
|  |  |  |  | 3、Concentration |  | 10-12secs | Stop watch and No.5 glass |  | Once/day | Worker leader |  | Shell temperature, humidity and thick liquid concentration check list |  | 3-08-005 |
| 10 | Wax removal |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 11 | Open furnace and material analysis |  |  | 1、Shell Physics test |  | No | No |  | Process control chart | Worker leader |  | No |  | 2-08-002 |
|  |  |  |  | 2、Temperature of pouring |  | Process control chart | Temperature tester |  | Per furnace | Worker |  | Process control chart |  | Process control chart |
|  |  |  |  | 3、Material analysis |  | As per specification | Spectrometer |  | Per furnace | QC |  | Spectrometer list |  | 3-08-006 |
| 12 | Casting shake out Marking & tracking |  |  | Heat No. |  | Clear, Correct | Visual |  | Per furnace | Worker |  | 4-10-004 |  | 3-07-001 |
| 13 | Sand blasting |  |  | Surface roughness |  | Smooth | Visual |  | Full | Worker |  | No |  |  |
| 14 | Gate cut off、Heat treatment、Physics property test |  |  | 1、Heat treatment |  | As per specification | Microscope |  | As per customer’s request | QC |  | Heat treatment report |  | 3-08-008 |
|  |  |  |  | 2、Physics property |  | As per specification | Tensile and Impact tester |  | As per customer’s request | QC |  | Tensile and impact report |  | 3-08-006 |
| 15 | Grinding |  |  | In gate grinding |  | Moderate height | Visual |  | Full | Worker |  | No |  |  |
| 16 | Acid wash |  |  | Change acid liquid |  | Shine | Visual |  | Daily | Worker |  |  |  | 4-08-006 |
| 17 | Final Inspection |  |  | 1、Appearance of casting |  | Clean, complete | Visual |  | Full | QC |  | Final inspection daily report |  |  |
|  |  |  |  | 2、Internal of casting |  | No shrinkage and defect | Visual |  | Full | QC |  | Final inspection daily report |  |  |
|  |  |  |  | 3、Letters of heat no. |  | Correct and Complete | Visual |  | Full | QC |  | Final inspection daily report |  | Process control chart |
|  |  |  |  | 4、Dimensions check |  | As per customer’s drawing | Caliper and Height gage |  | As per customer’s request or new molding | QC |  | 4-10-002 |  | Customer’s drawing and Incoming material inspection control standard |
|  |  |  |  | 5、P.T. |  | DIN 1690-2 | P.T. reagent |  | As per customer’s request | QC |  | 4-10-005 |  | DIN 1690-2 |
|  |  |  |  | 6、X-ray |  | DIN 1690-2 | X-ray tester |  | As per customer’s request | QC |  | 4-10-006 |  | DIN 1690-2 |
| 18 | Repair |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 19 | Packing and Delivery |  |  |  |  |  |  |  |  |  |  |  |  |  |